(Attention Specifiers, all areas in red require you to make selection based on requirements of the project before issuing specification. Please refer to the appropriate product data page when making your selection. All data pages are available at https://acousticalsolutions.com/)

# RECOMMENDED SPECIFICATION FOR ALPHASORB® ACOUSTIC FOAM BASS TRAP

# PART 1	GENERAL

## 1.01	SUMMARY

Section includes sound-absorptive bass traps.

Furnish and install bass traps and associated installation accessories as shown on the drawings, and specified herein, or as required to complete the work.

Related Documents: This section applies to drawings and general provisions of the subcontract. Review these documents for coordination with additional requirements and information that apply to work under this Section. Cross-reference approved supplementary manufacturers’ bass traps and required installation accessories including, but not limited to construction-grade adhesive, wall angle moldings, z-clips, z-bars, Velcro, or magnetic strips, as applicable.

## 1.02	REFERENCES

- American Society for Testing and Materials (ASTM) International:

ASTM C 423 Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

ASTM E 84 Standard Test Method for Surface Burning Characteristics of Building Materials.

ASTM E 795 Standard Practices for Mounting Test Specimens During Sound Absorption Tests.

ASTM E 336 Standard Test Method for Measurement of Airborne Sound Insulation in Buildings.

International Building Code.

L.E.E.D. - Leadership in Energy and Environmental Design is a set of rating systems for the design, construction, operation, and maintenance of green buildings

## 1.03	SYSTEM DESCRIPTION

- Performance Requirements

- Acoustical Absorption:  Perform testing in accordance with ASTM C 423 Type A mounting method unless otherwise specified.

Flame Spread Rating:  Provide all components with Class A flame spread rating when tested in accordance with ASTM E 84, unless otherwise specified.

## 1.04	SUBMITTALS

- Product Data: Manufacturer’s technical data for bass traps including fire-resistive characteristics, finishes, details of installation, and the following:

- Manufacturer's installation instructions.

Manufacturer’s SDS Sheets.

Certified laboratory test reports indicating compliance with Performance Requirements specified herein.

Samples:  Provide melamine foam sample of desired thickness of the following specified units for color selection or verification.

Shop Drawings: Layout and details of bass traps provided by qualified engineer or consultant, based on performance of proposed products. Show locations of items which are to be coordinated with, or supported by the structural ceiling and walls, if applicable.

Closeout Submittals:

- Operating and Maintenance Manual, including cleaning and maintenance instructions.

Extra Material for Owner’s stock.

Manufacturer’s Safety Data Sheets (SDS).

## 1.05	QUALITY ASSURANCE

- Single-Source Responsibility: Acoustical Solutions to provide bass traps (only).

Installer Qualifications: Acceptable to the manufacturer of the bass traps being installed. Utilize an installer having demonstrated 5 years minimum experience on projects of similar size and acoustical complexity.

Mock-Up:  Provide a mock-up for evaluation of installed appearance.

- Install panels in areas designated by proper authority.

Do not proceed with remaining work until proper authority approves workmanship and appearance.

Approved mock-up may remain as part of the work.

SURFACE BURNING CHARACTERISTICS

- Tested in accordance with ASTM E 84 - Fire rating Class A

Flame Spread Index ≤25

Smoke Developed Index ≤50

## 1.06	DELIVERY, STORAGE, AND HANDLING

- Delivery: Deliver material in the manufacturer’s original, unopened, undamaged containers with identification labels intact.

Provide labels indicating Acoustical Solutions brand name, style, size, and thickness.

Storage and Protection: Comply with manufacturer’s recommendations. Store acoustical product indoors and protected from exposure to harmful environmental conditions and at temperature and humidity conditions recommended by the manufacturer.

Wear handling gloves at all times when handling melamine foam-based products.

## 1.07	PROJECT CONDITIONS

- Environmental Limitations

- Install bass traps only in conditions that are within the manufacturer’s published limits for temperature and humidity.

Maintain the following conditions in areas where acoustical materials are to be installed 24 hours before, during and after installation:

- Relative Humidity: 25– 50%.

Uniform Temperature: 55–70 degrees F (13–21 degrees C).

Areas receiving panels should be free of construction debris and dust.

Mechanical, sprinkler and electrical trades shall have completed their work above the ceiling structure and within structural walls prior to commencement of product installation.

## 1.08	MAINTENANCE

- Extra Materials: Only if required for use by owner or the building maintenance and repair.

Provide new unopened cartons of extra materials, packaged with protective covering for storage and identified with appropriate labels

## 1.09	WARRANTY

- One-year limited warranty from invoice date for defects in workmanship or material.

Warranty excludes normal wear and tear, misuse, improper installation, and external damage.

Extended warranties are available for designated products.

# PART 2	PRODUCTS

## 2.01	MANUFACTURER

- Acoustical Solutions

- Contact: Acoustical Solutions, 3017 Vernon Road, Richmond, VA 23228; Telephone: (800) 782-5742; Email: info@acousticalsolutions.com; Website: AcousticalSolutions.com.

Substitutions: Not Permitted.

Provide all acoustical products specified herein by a single manufacturer.

## 2.02	MATERIALS

- Acoustical Solutions AlphaSorb Acoustic Foam Bass Traps. Bass traps are manufactured from 100% open-cell melamine foam with the following characteristics:

- Fire Resistance: ASTM E 84, Class A

AlphaSorb Natural White:

- Flat NRC: 1.60 per ASTM C423 Type J mounting

Convoluted A-12 NRC: 1.10 per ASTM C423 Type J mounting

AlphaSorb Natural White Bass Traps should achieve the following total absorption:

| Flat |  |  |  |  |
| --- | --- | --- | --- | --- |
| Specimen Absorption |  |  | Apparent Absorption Coefficient From Total Chamber Surface Area Covered | Apparent Absorption Coefficient from Total Exposed Surface Area |
| Freq. (Hz) | Sabins | Sabins/Unit |  |  |
| 31.5 | 12.70 | 1.59 | 0.20 | 0.24 |
| 40 | 4.79 | 0.60 | 0.07 | 0.09 |
| 50 | 5.90 | 0.74 | 0.09 | 0.11 |
| 63 | 14.19 | 1.77 | 0.22 | 0.27 |
| 80 | 16.13 | 2.02 | 0.25 | 0.30 |
| 100 | 21.68 | 2.71 | 0.34 | 0.41 |
| 125 | 45.73 | 5.72 | 0.71 | 0.86 |
| 160 | 74.34 | 9.29 | 1.16 | 1.40 |
| 200 | 103.07 | 12.88 | 1.61 | 1.95 |
| 250 | 101.19 | 12.65 | 1.58 | 1.91 |
| 315 | 100.77 | 12.60 | 1.57 | 1.90 |
| 400 | 97.68 | 12.21 | 1.53 | 1.84 |
| 500 | 96.05 | 12.01 | 1.50 | 1.81 |
| 630 | 89.49 | 11.19 | 1.40 | 1.69 |
| 800 | 84.27 | 10.53 | 1.32 | 1.59 |
| 1,000 | 77.04 | 9.63 | 1.20 | 1.45 |
| 1,250 | 73.60 | 9.20 | 1.15 | 1.39 |
| 1,600 | 70.35 | 8.79 | 1.10 | 1.33 |
| 2,000 | 65.75 | 8.22 | 1.03 | 1.24 |
| 2,500 | 61.26 | 7.66 | 0.96 | 1.16 |
| 3,150 | 58.72 | 7.34 | 0.92 | 1.11 |
| 4,000 | 57.06 | 7.13 | 0.89 | 1.08 |
| 5,000 | 58.25 | 7.28 | 0.91 | 1.10 |
| 6,300 | 56.70 | 7.09 | 0.89 | 1.07 |
| 8,000 | 57.61 | 7.20 | 0.90 | 1.09 |
| 10,000 | 55.30 | 6.91 | 0.86 | 1.04 |
| 12,500 | 53.70 | 6.71 | 0.84 | 1.01 |
| Apparent NRC: |  |  | 1.35 | 1.60 |
| Apparent SAA: |  |  | 1.33 | 1.61 |

| Convoluted |  |  |  |  |
| --- | --- | --- | --- | --- |
| Specimen Absorption |  |  | Apparent Absorption Coefficient From Total Chamber Surface Area Covered | Apparent Absorption Coefficient from Total Exposed Surface Area |
| Freq. (Hz) | Sabins | Sabins/Unit |  |  |
| 31.5 | 13.19 | 1.65 | 0.21 | 0.16 |
| 40 | 3.21 | 0.40 | 0.05 | 0.04 |
| 50 | 1.94 | 1.37 | 0.17 | 0.14 |
| 63 | 14.23 | 1.78 | 0.22 | 0.18 |
| 80 | 17.65 | 2.21 | 0.28 | 0.22 |
| 100 | 23.23 | 2.90 | 0.36 | 0.29 |
| 125 | 48.79 | 6.10 | 0.76 | 0.61 |
| 160 | 73.68 | 9.21 | 1.15 | 0.92 |
| 200 | 105.13 | 13.14 | 1.64 | 1.31 |
| 250 | 107.86 | 13.48 | 1.69 | 1.35 |
| 315 | 110.45 | 13.81 | 1.73 | 1.38 |
| 400 | 104.32 | 13.04 | 1.63 | 1.30 |
| 500 | 100.65 | 12.58 | 1.57 | 1.26 |
| 630 | 95.19 | 11.90 | 1.49 | 1.19 |
| 800 | 84.83 | 10.60 | 1.33 | 1.06 |
| 1,000 | 78.14 | 9.77 | 1.22 | 0.98 |
| 1,250 | 73.77 | 9.22 | 1.15 | 0.92 |
| 1,600 | 71.68 | 8.96 | 1.12 | 0.90 |
| 2,000 | 67.23 | 8.40 | 1.05 | 0.84 |
| 2,500 | 63.33 | 7.92 | 0.99 | 0.79 |
| 3,150 | 60.62 | 7.58 | 0.95 | 0.76 |
| 4,000 | 59.43 | 7.43 | 0.93 | 0.74 |
| 5,000 | 59.84 | 7.48 | 0.94 | 0.75 |
| 6,300 | 58.92 | 7.37 | 0.92 | 0.74 |
| 8,000 | 59.83 | 7.48 | 0.93 | 0.75 |
| 10,000 | 62.28 | 7.79 | 0.97 | 0.78 |
| 12,500 | 61.96 | 7.74 | 0.97 | 0.77 |
| Apparent NRC: |  |  | 1.40 | 1.10 |
| Apparent SAA: |  |  | 1.38 | 1.11 |

Foam Density:

- Natural Light Grey: 0.56 lbs./ft³ +/- 0.09 lbs./ft³

Natural White: 0.47lbs./ft³ +/- 0.13lbs./ft³

Service Temperature: -40˚F to 350˚F

Size: Nominal: 12 inches x 12 inches (610 mm x 610 mm) x 24 inches or 48 inches tall

Panel Total Thickness: Nominal 8-3/8 inches (213mm). Other thicknesses available upon request.

Manufacturers Standard Textiles/Colors: Available upon request

## 2.03	ACCESSORIES

- Bass Traps

- Instant grab, high strength construction adhesive such as Power Grab by Loctite.

Two-part Z-clips: Manufacturer’s standard mounting bar and matching clips for mounting on rear of bass traps.

Wall angle moldings, impaling clips, Z-channel, Velcro and magnetic strips provided by others.

# PART 3	EXECUTION

## 3.01	EXAMINATION

Examine bass trap installation, with installer present, for compliance with requirements specified in this and other applicable Sections affecting product installation and with requirements for installation tolerances and other conditions affecting performance of the selected Acoustical Solutions product.

## INSTALLATION

- Do not begin installation until materials sufficient to complete an entire room are received and prepared for installation.

Symmetrically locate product layout, as desired, in each space. Coordinate work with other trades so that lighting fixtures, HVAC and other ceiling and/or wall mounted fixtures work with bass trap installation.

Install materials in accordance with manufacturer's printed instructions and to comply with governing regulations, fire resistance rating requirements as indicated and industry standards applicable to the work.

Take care not to damage or mark the product; wear clean cotton or canvas gloves and avoid the use of latex gloves.

## 3.03	CLEANING

- Clean exposed surfaces of acoustical product and any installation accessories to comply with manufacturer’s instructions for cleaning.

Touch up any minor finish damage.

Remove and replace work that cannot be successfully cleaned and repaired to permanently eliminate evidence of damage.

## 3.04	PROTECTION

- Protect installed products until completion of project.

# END OF SECTION