PAGE  
[image: image1.png]


SPECIFICATION               SECTION 03 54 00
[image: image2.png]BENEATH IT ALL, MAXXON DELIVERS.





RECOMMENDED SPECIFICATION FOR MAXXON COMMERCIAL LEVEL EZ FLOOR UNDERLAYMENT FOR TOPPING CONCRETE
PART 1 GENERAL

1.01    SUMMARY

A. Description of Work: Work of this section includes underlayment for interior finish flooring over cast in place concrete, precast or hollowcore plank concrete, and is not limited to the following:

1. Maxxon® Commercial Level EZ™ Floor Underlayment covering normal project conditions and applications.

2. Division 3 Section-Concrete: “Cast Underlayment” 
1.02 REFERENCES
A. Underwriters Laboratory 

Fire Resistance Volume 1

www.ul.com
B. ASTM C109M


Standard Test Method for Compressive Strength of 




Hydraulic Cement Mortars

C. ASTM F2170



Standard Test Method for Determining Relative





Humidity in Concrete Floor Slab

D. ASTM F2873



Standard Practice for the Installation of Self-Leveling 




Underlayment and Preparation of Surface to Receive 




Resilient Floor Goods
E. ASTM F2678



Standard Practice for Preparing Panel Underlayments, 

Thick Poured Lightweight Cellular Concrete Underlayments, and Concrete Subfloors with Underlayment Patching Compounds to Receive Resilient Flooring

F. TCNA F 180/F200



Tile Council of North America Installation Handbook

www.tileusa.com
G. NWFA




National Wood Flooring Association Instructions

www.nwfa.org
H. Finished Floor Goods Procedures
Maxxon Procedures for Attaching Finished Floor





Goods to Maxxon Underlayments

www.maxxon.com
1.03    SUBMITTALS

A. Product Data: Submit sale sheets Maxxon® Commercial Level EZ™ Technical Data Sheet, Procedures for Attaching Finished Floor Goods to Maxxon Underlayments, and Maxxon’s Building Conditions Guide with project materials clearly identified for each required product or system.
B. UL Directory Fire Resistance Volume 1 – See www.maxxon.com for the current list of applicable UL or ULC fire designs.
       

C. Code Approvals: See www.maxxon.com for the current list of code approvals.

1.04     SYSTEM REQUIREMENTS

A. Performance Requirements:

1. Maxxon® Commercial Level EZ™ Floor Underlayment 

Compressive Strength (Modified ASTM C109):
1,250 psi (8.6 MPa) 24 hours

2,700 psi (18.6 MPa) 7 days

Minimum 5,000 psi (34.5 MPa) at 28 days
1.05    QUALITY ASSURANCE

A. Performance Standards:

1. All materials, unless otherwise indicated, shall be manufactured by Maxxon Corporation and shall be installed in accordance with its current printed directions and by a Maxxon Corporation Authorized Applicator.

2. Underlayment mix shall be tested for a slump using a 2" (i.d.) x 4" (50 mm x 101 mm) cylinder and an acrylic or plexiglass sheet resulting in a patty size of 11 ½ inches (292 mm) plus or minus 1 inch (25 mm) diameter.
3. Compressive strength tested in accordance with ASTM C109M.

1.06    DELIVERY, STORAGE AND HANDLING

A. All materials shall be delivered in their original unopened packages and protected from damage and exposure from the elements. Damaged or deteriorated materials shall be removed from the premises.

1.07    PROJECT CONDITIONS

A. Before, during and after installation of product, building interior shall be enclosed, with adequate ventilation and heat maintained at a temperature above 50 °F (10 °C) to allow for drying of product.

PART 2 GENERAL

2.01    PRODUCTS AND MANUFACTURERS

      A.  Manufacturer: Maxxon Corporation, Hamel, MN Telephone: (800) 356-7887.  
2.02    MATERIALS

A. Proprietary products/systems: Poured flooring underlayment and topping products, including the following:

1. Maxxon® Commercial Level EZ™ Floor Underlayment
B. Maxxon Floor Primer:

1. Material Standard: Comply with specifications outlined in manufacturer's Design and Installation.

C. Mix Water:

1. Material Standard: Potable, free from impurities and from a domestic source.

D. Maxxon Commercial Multi-Use Acrylic Primer:
1. Seal all areas that receive glue down floor goods with Maxxon Commercial Multi-Use Acrylic Primer according to manufacturer’s specifications.
PART 3 EXECUTION

3.01    EXAMINATION

A. Site Verification of Conditions:
1. Installation shall not begin until the building is enclosed, including roof, windows, doors, and any other apertures.
2. Concrete substrate shall be structurally sound, properly fastened and dry. Contractor shall clean subfloor to remove mud, oil, grease and construction debris before arrival of the authorized applicator.

3. Maxxon® Commercial Level EZ™ is not a vapor barrier. The general contractor, architect, specifier, or building owner shall test below grade, on grade, or elevated slabs for MVER (ASTM F1869-16) or RH (ASTM F2170). If the MVER or RH of the concrete substrate exceeds the floor covering manufacturer’s respective requirements for the finished floor system, the concrete should be treated with a moisture vapor barrier, such as Maxxon MVP One or MVP Two, before installing Level-One EZ.

3.02    REQUIREMENTS

A. Leak Prevention:

1. Fill cracks and voids in subfloor where leakage of slurry could occur.

B. Priming subfloor:  
1. Prime substrate according to manufacturer's recommendations. 

C. Application:

1. Install in accordance with reference standards and manufacturer's instructions.
3.03    GENERAL INSTALLATION REQUIREMENTS

A. Mixing Proportions:

1. General Requirements: Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

B. Application:

1. Pour floor topping to recommended thickness. Immediately spread and screed product to a smooth surface.  Expansion joints in all types of work shall be brought through the underlayment.

i) Recommended Minimum Maxxon® Commercial Level EZ™ Underlayment Depth 1/4” – 2” (6 – 51 mm).
C. Drying:

1. The general contractor must provide and maintain correct environmental conditions to keep the building clean and dry, and protect against infestation of moisture from a variety of potential sources.  The general contractor must supply mechanical ventilation and heat if necessary to remove moisture from the area until the Maxxon® Commercial Level EZ™ is dry. 

2. Protection from Heavy Loads:  During construction, place temporary wood planking over Maxxon® Commercial Level EZ™ wherever it will be subject to heavy wheeled or concentrated loads. 
3.04 PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Sealing:  

1. Seal all areas that receive glue down floor goods with Maxxon Commercial Gypsum Overspray or Maxxon Commercial Multi-Use Acrylic Primer according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.
2. Maxxon Commercial Fortify can be used over Maxxon underlayments in low traffic areas such as utility rooms, storage rooms and closets, as a protective surface.
B. Moisture Testing:

1. Follow the respective floor goods manufacturers’ recommendations for relative humidity requirements.  When manufacturer does not have a relative humidity requirement, refer to Maxxon’s Procedures for Attaching Finished Floor Goods to Maxxon Underlayments brochure.   
C. Finished Floor Goods:

1. There are many reference standards for the installation procedures and recommendations for finished flooring applications over gypsum underlayments.  These include instructions of the manufacturers of the finished flooring, adhesives and thin-set as well as national agency reference standards.  The national standards are listed below: 

	Flooring Type
	Reference Standard

	Resilient 
	ASTM F2873

	Ceramic Tile
	TCNA F180/F200

	Wood
	NWFA Instructions


See Maxxon Corporation's Procedures for Attaching Finished Floor Goods to Maxxon Underlayments brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.  

END OF SECTION
