PAGE  
[image: image1.png]


SPECIFICATION         SECTION 03 54 00
[image: image2.png]BENEATH IT ALL, MAXXON DELIVERS.





HYDRAULIC CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR MAXXON COMMERCIAL PRO LEVEL-RIGHT SELF-LEVELING FLOOR UNDERLAYMENT OVER MAXXON COMMERCIAL LOW DENSITY FILL 
PART 1 GENERAL

1.01    SUMMARY

A. This is the recommended specification for Maxxon® Commercial Pro Level-Right® over Maxxon® Commercial Low Density Fill:
1. Maxxon® Commercial Pro Level-Right® Floor Underlayment covering normal project conditions and applications.

2. Division 3 Section-Concrete: “Cast Underlayment”
3. Division 9 Section-Finishes: “Acoustic Treatment”

1.02 REFERENCES

A. Underwriters Laboratory 
Fire Resistance Volume 1






www.ul.com
B. ASTM E336 and E1007
Field Sound Transmission Class (F-STC), Field

Impact Insulation Class (F-IIC)

C. ASTM E90 and E492
Sound Transmission Class (STC), Impact

Insulation Class (IIC)

D. GREENGUARD Certified
GREENGUARD Certified and GREENGUARD Gold Certified



www.greenguard.org
E. ASTM C109M

Standard test method for compressive strength of Hydraulic
Cement mortars

F. ASTM F2170


Standard Test Method for Determining Relative

Humidity in Concrete Floor Slab. See Section 3.01 EXAMINATION.
G. ASTM F2678
Standard Practice for Preparing Panel Underlayments, Thick Poured Gypsum Concrete Underlayments, Thick Poured Lightweight Cellular Concrete Underlayments, and Concrete Subfloors with Underlayment Patching Compounds to Receive Resilient Flooring

H. TCNA F 180/F200


Tile Council of North America Installation Handbook

www.tileusa.com
I. NWFA



National Wood Flooring Association

Instructions

www.nwfa.org
J. Procedures Guide

Maxxon Procedures for Attaching Finished Floor

Goods to Maxxon Underlayments

www.maxxon.com
1.03    SUBMITTALS

A. Product Data: Submit sale sheets Maxxon® Commercial Pro Level-Right® Sales Sheet, Low Density Fill Spec Sheet, Acousti-Mat TDS, Acousti-Mat Perimeter Isolation Strip Spec Sheet, Procedures for Attaching Finished Floor Goods to Maxxon Underlayments, and Maxxon’s Building Conditions Guide with project materials clearly identified for each required product or system.
B. Acoustical Data: Submit sound tests according to IBC code criteria ASTM E492 (IIC) and ASTM E90 (STC) or ASTM E1007 (F-IIC) and E336 (F-IIC).

C. Code Approvals: See www.maxxon.com for the current list of code approvals.
1.04     SYSTEM REQUIREMENTS

A. Performance Requirements:

1. Maxxon® Commercial Pro Level-Right® Floor Underlayment (An Eco-Friendly building product)
i) Compressive Strength (Modified ASTM C109):
ii) Typical range of 5,000 – 7,000 psi (34.5 – 48.3 MPa)
iii) Density 115-125 pounds per cubic foot (1842-2,002 kg/m3)
2. Maxxon® Commercial Low Density Fill 
i) Compressive Strength (Modified ASTM C109):
ii) Typical range of 200 - 500 psi (1.38 - 3.45 MPa)2
iii) Density 28-32 pounds per cubic foot (449 – 513 kg/m3)
*****This product may help contribute toward USGBC LEED Credits (MR 3; EQ 2, 4)*****

Potential USGBC LEED Credit Contribution:


  a. MR Credit 3: Building Product Disclosure and Optimization - Sourcing Raw Material

  b. EQ Credit 2: Low Emitting Materials.


  c. EQ Credit 4: Indoor Air Quality Assessment.


Contact Maxxon Corporation for specific details.

******************************************************************************************************

1.05    QUALITY ASSURANCE

A. Performance Standards:

1. All materials, unless otherwise indicated, shall be manufactured by Maxxon Corporation and shall be installed in accordance with its current printed directions and by a Maxxon Corporation Authorized Applicator.

2. Underlayment mix shall be tested for a slump using a 2" (i.d.) x 4" (50 mm x 101 mm) cylinder resulting in a patty size of 9 ½ (241 mm) inches plus or minus 1 inch (25 mm) diameter.
3. Compressive strength tested in accordance with ASTM C109M.

1.06     DELIVERY, STORAGE AND HANDLING

       A.  All materials shall be delivered in their original unopened packages and protected from damage and exposure from the elements. Damaged or deteriorated materials shall be removed from the premises.

1.07     PROJECT CONDITIONS

      A.   Before, during and after installation of product, building interior shall be enclosed, with adequate ventilation and heat maintained at a temperature above 50 °F (10 °C) to allow for drying of product.
PART 2 GENERAL

2.01     PRODUCTS AND MANUFACTURERS

      A.  Manufacturer: Maxxon Corporation, Hamel, MN. Telephone: (800) 356-7887
2.02    MATERIALS

A. Proprietary products/systems: Poured flooring underlayment, fill products and topping products, including the following:

1. Maxxon® Commercial Pro Level-Right® Floor Underlayment
2. Maxxon® Commercial Low Density Fill
B. Proprietary products/systems: Optional Sound Control that does not negate the fire rating and is specified in UL design. Acoustical performance is dependent on system design and construction.
1. Maxxon Acousti-Mat® 1/8 Sound Mat


2. Maxxon Acousti-Mat® 1/4 Sound Mat

3. Maxxon Acousti-Mat® 1/4 Premium Sound Mat

4. Maxxon Acousti-Mat® 3/8 Sound Mat

5. Maxxon Acousti-Mat® 3/8 Premium Sound Mat

6. Maxxon Acousti-Mat® 3/4 Sound Mat

7. Maxxon Acousti-Mat® 3/4 Premium Sound Mat

***********These products may contribute to USGBC LEED Credits (EQ 2, 4, 9)***********
Potential USGBC LEED Credit Contribution:


  a. EQ Credit 2: Low Emitting Materials.


  b. EQ Credit 4: Indoor Air Quality Assessment.


  c. EQ Credit 9: Acoustic Performance.


Contact Maxxon Corporation for specific details.

******************************************************************************************************

C. Maxxon Acousti-Mat Perimeter Isolation Strips as manufactured by Maxxon Corporation, Hamel, MN
D. Maxxon Acousti-Mat Tape as manufactured by Maxxon Corporation, Hamel, MN
E. Maxxon Commercial Gypsum Overspray or Maxxon Commercial Multi-Use Acrylic Primer:

1. Material Standard: Comply with recommendations as per Maxxon Corporation
F. Mix Water:

1. Material Standard: Potable, free from impurities and from a domestic source.

G. Sand Aggregate:

1. Sand shall meet Maxxon Sand Specification 101.
H. Maxxon® Commercial Low Density Fill: 

1. Lightweight Portland cement and coated expanded polystyrene foam aggregate product.
I. Maxxon Commercial Gypsum Overspray:

1. Seal all areas that receive glue down floor goods with Maxxon Commercial Gypsum Overspray according to manufacturer's specifications.

J. Maxxon Commercial Multi-Use Acrylic Primer (Alternate to Overspray):
1. Seal all areas that receive glue down floor goods with Maxxon Commercial Multi-Use Acrylic Primer according to manufacturer’s specifications.
K. Maxxon Reinforcement

PART 3 EXECUTION

3.01     EXAMINATION

A. Site Verification of Conditions:
1. Installation shall not begin until the building is enclosed, including roof, windows, doors, and any other apertures.
2. Wood substrate shall be structurally sound, properly fastened, and dry. Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before arrival of the authorized applicator.

3. Wood substrate:

i) The wood subfloor must be adequate to withstand live and dead loads with a deflection limitation of L/360.

ii) Wood should be agency approved 23/32” (1.8 cm) T & G subfloor sheathing.
4. Concrete substrate:

i) The concrete substrate shall be structurally sound, properly fastened and dry. Contractor shall clean subfloor to remove mud, oil, grease and construction debris before arrival of the authorized applicator.

5. Maxxon® Commercial Pro Level-Right® and Maxxon® Commercial Low Density Fill are not vapor barriers. The general contractor, architect, specifier, or building owner shall test below grade, on grade, or elevated slabs for MVER (ASTM F1869-16) or RH (ASTM F2170). If the MVER or RH of the concrete substrate exceeds the floor covering manufacturer’s respective requirements for the finished floor system, the concrete should be treated with a moisture vapor barrier, such as Maxxon MVP One or MVP Two before installing Maxxon® Commercial Pro Level-Right® and Maxxon® Commercial Low Density Fill.
3.02     REQUIREMENTS

A. Leak Prevention:

1. Fill cracks and voids in subfloor where leakage of slurry could occur.
B. Prime subfloor prior to installation of Maxxon® Commercial Low Density Fill according to manufacturer’s recommendations.
C. Install Maxxon® Commercial Low Density Fill.
D. Priming Maxxon® Commercial Low Density Fill:  
1. Prime Maxxon® Commercial Low Density Fill with Maxxon Commercial Gypsum Overspray or Maxxon Commercial Multi-Use Acrylic Primer according to manufacturer recommendations. 

E. Application:

1. Install in accordance with reference standards and manufacturer's instructions.
3.03    GENERAL INSTALLATION REQUIREMENTS

A. Day 1 – Application (Maxxon® Commercial Low Density Fill): 
1. (Optional) Acousti-Mat Installations:  Install Acousti-Mat following manufacturer’s recommendations and specifications including installation of Perimeter Isolation Strips at the perimeter of all areas receiving Acousti-Mat (including doorframes) and around any protrusions through the installation.  Adhere the foam perimeter isolation strip to the wall with Acousti-Mat Tape.
2. Depending on deep-fill criteria: Set eyelets on finishing rake to desired thickness, or set grade pins, or pull string lines to desired thickness. Install a minimum ½” to desired thickness of Maxxon® Commercial Low Density Fill according to manufacturer recommendations.
B. Day 2 – Application (Maxxon® Commercial Pro Level-Right®)

1. Install Maxxon® Commercial Pro Level-Right® at a minimum of ¾”.
C. Mixing Proportions:

1. General Requirements: Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.
D. Drying:

1. The general contractor must provide and maintain correct environmental conditions to keep the building clean and dry, and protect against infestation of moisture from a variety of potential sources.  The general contractor must supply mechanical ventilation and heat if necessary to remove moisture from the area until the Maxxon® Commercial Pro Level-Right® is dry. 

2. Protection from Heavy Loads:  During construction, place temporary wood planking over Maxxon® Commercial Pro Level-Right® wherever it will be subject to heavy wheeled or concentrated loads.

3.04 PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

A. Sealing:  

1. Seal all areas that receive glue down floor goods with Maxxon Commercial Gypsum Overspray or Maxxon Commercial Multi-Use Acrylic Primer according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.
2. Maxxon Commercial Fortify can be used over Maxxon underlayments in low traffic areas such as utility rooms, storage rooms and closets, as a protective surface.
B. Moisture Testing:

1. Follow the respective floor goods manufacturers’ recommendations for relative humidity requirements.  When manufacturer does not have a relative humidity requirement, refer to Maxxon’s Procedures for Attaching Finished Floor Goods to Maxxon Underlayments brochure.   
C. Finished Floor Goods:

1. There are many reference standards for the installation procedures and recommendations for finished flooring applications over floor underlayments.  These include instructions of the manufacturers of the finished flooring, adhesives and thin-set as well as national agency reference standards.  The national standards are listed below: 

	Flooring Type
	Reference Standard

	Resilient 
	ASTM F2873

	Ceramic Tile
	TCNA F180/F200

	Wood
	NWFA Instructions


See Maxxon Corporation's Procedures for Attaching Finished Floor Goods to Maxxon Underlayments brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.  

END OF SECTION
