(Attention Specifiers, all areas in red require you to make selection based on requirements of the project before issuing specification. Please refer to the appropriate product data page when making your selection. All data pages are available at https://acousticalsolutions.com/)

# RECOMMENDED SPECIFICATION FOR
PRIVACYSHIELD® AQFA-10EXT EXTERIOR SOUNDPROOFING BLANKETS

# PART 1	GENERAL

## 1.01	SUMMARY

This section includes the following:

Exterior Grade noise control curtains (sound curtains) for permanent or long-term projects

## 1.02	SUBMITTALS

- Shop drawings: show fabrication and installation details for acoustical panels, including grommet location.

Submittals: Furnish 18" X 21" samples for quality and general panel construction.

Technical data sheets reflecting construction, panel thickness, weight, and Acoustical data.

## 1.03	DELIVERY, STORAGE AND HANDLING

- Deliver in unopened skids and store in a dry place with adequate air circulation. Store materials such that they will be free from accidental damage.

## 1.04	WARRANTY

- One-year limited warranty from invoice date for defects in workmanship or material.

Warranty excludes normal wear and tear, misuse, improper installation, and external damage.

Extended warranties are available for designated products.

# PART 2	PRODUCTS

## 2.01	SOUND CURTAINS, GENERAL

- Sound Curtains shall consist of a nominal 2” thick quilted fiberglass sound absorber faced on both sides with an exterior grade facing.

- Products

Model # AQFA-10EXT
Acoustical Solutions
3017 Vernon Road
Richmond, VA 23228
PH: 800-782-5742
AcousticalSolutions.com

Exterior grade facing material:

- Shall be a heavy duty 8 oz./yd2 PVC polyester fabric facing

Shall be mechanically attached to the fiberglass by a quilting process

Quilted fiberglass:

- Shall be nominal 2" thick

Shall have a nominal density of 2.0 lb/ft3

Sound Absorption Coefficient of 0.94 @ 250 Hz

Standard Width: 48 inches

Length: As indicated, up to 25 feet long

## 2.02	CONSTRUCTION

- Sound curtain panels or rolls shall be supplied in sizes indicated.  Manufacturers standard panel construction shall have all edges bound and #4 spur grommets across the top & bottom.

- All edges bound and be sewn to the barrier with a Tenara exterior grade thread.

## 2.03	MOUNTING

- Manufacturer’s standard accessories for securely mounting the sound curtain panels:

- Grommets may be installed at the top and bottom of each panel to facilitate mounting.

- On panels over 1'" long an additional row of double grommets may be installed across the middle of the panel

- Mechanical fastener to be installed through the grommets in the panel(s) into the support structure or wall.

- Place a large fender washer with a center hole ID smaller than that of the mechanical fastener head, on top of the grommet you are securing through.

- Or Battens can be used

- Place a batten system along the top and bottom of the panels

Using a mechanical fastener that is appropriate for the substrate secure directly through the batten and acoustical composite into the support structure or wall

Place a vertical batten on any columns or vertical supports and secure battens into place around the entire perimeter of the structural support or wall using the method above.

If necessary, you may use a mechanical fastener to temporarily hold the panels in place while installing the battens

- Continue in this manner until the entire sound curtain wall is erected or the entire wall surface is covered.

## 2.04	ACOUSTICAL PERFORMANCE

Sound Absorption: Per ASTM C423

Octave Band Center Frequency (Hz)

125	250	500	1000	2000	4000	NRC

.46	.94	.85	.64	.47	.33	.75

# PART 3	EXECUTION

## 3.01	INSTALLATION

- Install sound curtain panels in locations indicated. Comply with manufacturer’s written instructions for installation by using type of mounting accessories indicated or, if not indicated, as recommended by the manufacturer.

## CLEANING

- After completion of installation of panels or rolled goods, remove dust and other foreign material according to manufacturer’s written instructions.

- Remove surplus material, rubbish, and debris resulting from quilted fiberglass absorber installation, on completion of work, and leave areas of installation in a neat and clean condition.

# END OF SECTION